## Slide 1: Study of spin dynamics in ferrite-based MNPs
Dott. Martina Basini
Supervised by: Alessandro Lascialfari

## Slide 2: OUTLINE
Introduction to nanomagnetism
SUPERPARAMAGNETIC nanoparticles (MNPs):
  Biomedical appications
  MNPs as theranostic agents
MY RESEARCH :
  Samples
  Magnetic measurement
  NMR Profiles
  Results
CONCLUSIONS and PERSPECTIVES

## Slide 3
Superparamagnetism
Ferromagnetism
SOME CRITICAL DIAMETER:
INTRODUCTION TO NANOMAGNETISM
All the spin move coherently
COMPETITION between ANISOTROPY and THERMAL ENERGY
Spins filipping in Nèel time
tN = t0(E) exp [DEa/Kb (T-T0)]
B = 0
Ea = Barrier
d < Dc

## Slide 4
SUPERPARAMAGNETIC NANOPARTICLES
  MAGNETIC CORE:
MAGHEMITE (γ-Fe2O3) /
MAGNETITE (Fe3O4)
HOW ARE MNPs MADE?
HYDROPHOBIC COATING:
OLEIC ACID
SOLVENT
HEXANE / ACQUEUS MEDIA
POSSIBILITY OF FUNCTIONALIZATION

## Slide 5
Proteins
Virus
Cells
0.1 nm
1 nm
10 nm
100 nm
1 m
10 m
100 m
Gene (width)
Bacteria
DNA
Human hair
pollen
Aspirin molecule
nanoparticles
SUPERPARAMAGNETIC NANOPARTICLES
WHY ARE THEY APPEALING FOR BIOMEDICAL APPLICATIONS?
DIMENSION
MAGNETIC TRANSPORT
CAN BE BIOCOMPATIBLE
POSSIBLE FUNCTIONALISATION

## Slide 6
DEPEND ON TRANSVERSE RELAXIVITY (PHYSICAL PROPERTY)
SUPERPARAMAGNETIC NANOPARTICLES
DIAGNOSTIC:
CONTRAST AGENT (CA)
FOR MRI
With CA
Without CA
THERANOSTIC AGENTS:
THERAPY:
MAGNETIC
FLUIDHYPERTEMIA
TARGETING:
DRUGS, ANTIBODY
THE IDEAL TASK: A single theranostic nano-object !!

## Slide 7: THE ROLE OF PHYSICIST
INVESTIGATION OF FUNDAMENTAL magnetic properties and relaxation rates’ mechanisms
CORRELATION
WITH APPLICATIVE properties
NMR
RELAXATION
DISPERSION CURVES
MAGNETIC MEASUREMENTS

## Slide 8: Few words on NMR TECHNIQUE
NMR
RELAXATION
NUCLEI
(T2n)
ELECTRONS
(T2e)
PHONONS
T1n
T1n
T1e
LOCAL HYPERFINE INTERACTION
BETWEEN NUCLEI AND ELECTRON
NOW (Mz = 0):
Start recording relaxation to equilibrium
B1
90° PULSE
1/T1n ATJe(ωN)
1/T2n  Je(0)
Electronic
spectral density
Je(ω) = FT [G(r , t)]
1H relaxation:
LOCAL PROBE through the
EYES of HF INTERACTION!!
Probe: 1H (high natural abundance)
Measure: relaxation time of 1H
ALONE THEY WOULD RELAX IN YEARS
Interacting with MNP’s THEY RELAX IN t < s

## Slide 9
The nanostructures we have studied contains surfactant-capped magnetite (Fe3O4) inorganic core with different controlled size ranging from 3.5 to 17.5 nm . The as-syntesized nanostructures are passivated by hydrophobic surfactants (oleic acid) and fully dispersed both in hexane and in acqueous media by means of microemulsions.
dcore = 4 nm
 = 0.15
dcore = 8.5 nm
 = 0.07
dcore = 20 nm
 = 0.09
L = 8.5 nm
A
B
C
D
Solvent: HEXAN
Solvent:
ACQUEOUS MEDIA
C_acq
D_acq
TEM
MY STUDY: SAMPLES
GOALS:
APPLICATIVE: IDENTIFY NEW possible MRI Contrast Agents
FUNDAMENTAL: Study of SPIN DYNAMICS

## Slide 10: MY STUDY: AC and DC Magnetic measurement
T < TB
TB
t = t0(E) exp [DEa/KB (T-T0)]
Max RESPONSE at
TMAX  TB
such that
ω  1
BLOCKING-SPIN TEMPERATURE
AC
DC
HYSTERESIS
Spins are bloked (H = 0 ; M  0)
Energy Barrer distribution
DEa
t0
T0
MEASURE THE INTERACTIONS
10 -10 - 10-12 s
B = 0
B ≠ 0
M

## Slide 11: MY STUDY: NMR relaxation curves
1H relaxation times
(T1 and T2) depend on the capability to
EXCHANGE ENERGY
with the sorrounding:
!! LOCAL PROBE !!
MNPs shorten the relaxation time T2 of 1H of healty cells:
CONTRAST AGENTS
Key parameter for MNPs CA efficiency :
r2 ~ 1 / T2
Magnetic Resonant Imaging
MRI signal is:
s(t) = N(1H) e-TE/T2 (1-e-TR/T1)

## Slide 12
MY STUDY: NMR Results
Acqueus media
INCREASE CA EFFICIENCY
SPHERICAL SHAPE
4 nm promising as negative CA!!
SIZE
SOLVENT
SHAPE

## Slide 13: EXISTING MODELS….
...Work for r1…
...Don’t Work for r2..
FIT LINES

## Slide 14: CONCLUSIONS and PERSPECTIVES
SPHERICAL shape is better
d ~ 20 nm displays the BEST EFFICIENCY:
r2 = 50 s-1mM-1
d ~ 4 nm has r2 = 27 s-1mM-1, VERY HIGH with respect to the SMALL SIZE…
WE NEED A THEORY FOR BOTH r1 and r2 !!!
…further work is required