## Slide 1
18/11/2014
Physics, Astrophysics and Applied Physics PhD School
NANOMECHANICAL AND TOPOGRAPHICAL IMAGING OF LIVING CELLS AND TISSUES
FOR THE INVESTIGATION
OF CELLULAR INTERACTIONS
Luca Puricelli
Molecular Beam and Nanocrystalline Materials Laboratory (LGM)
Dipartimento di Fisica & Centro Interdisciplinare Materiali e Interfacce Nanostrutturati (CIMaINa)
Università degli Studi di Milano

## Slide 2
FUNDAMENTAL CONCEPTS
The Atomic Force Microscope (AFM)
Working principles
Nanostructured surfaces:
- Which are their main
features and purposes?
Cellular mechanics:
- How does a cell react
to its environment?
Induced cellular differentiation

## Slide 3: CELLULAR MECHANICS
Why measuring cells’ mechanical properties ?
Fluorescence microscopy image : endothelial cells
Structural role: scaffolding
Biological primary functions
Adhesion
Proliferation
Intra-cellular transport
Differentiation
Signals transduction
MECHANICAL PHENOTYPE
CELL’ S VITAL PARAMETERS
CYTOSKELETON
*
* E. L. Elson. Ann. Rev. Biophys. Chem (1988)

## Slide 4: CELLULAR MECHANICS
Cellular (or tissues) elasticity correlated to :
Environment physico-chemical variations **
Patho-physiological state
(even without clear morphological changes)*
* M. Plodinec . Nature Nanotech. (2012)
** G. Lamour. Biomat. (2010)

## Slide 5
NANOSTRUCTURED SURFACES
Flat
VS
Nanostructured
Different physical properties for the same material:
RMS roughness
electric charge density
Surface Free Energy, etc..
May an engineered nanostructured surface influence a cell’s fate?

## Slide 6
THE ATOMIC FORCE MICROSCOPE (AFM)
h ≈ 10 um
R ≈ 2-3 nm

## Slide 7
AFM & CELLS
AFM : COMBINED TOPOGRAPHIC/MECHANICAL IMAGING
Topographic maps
Height
nm
Mechanical tests:
(Force measurements)
Young Modulus

## Slide 8
AFM & CELLS : FORCE VOLUME
Force Volume :
- 100x100 μm2
64 x 64 force curves
ELASTICITY MAP
TOPOGRAPHY MAP
Sample deformation
Force [nN]
Tip-sample distance [nm]

## Slide 9
AFM & CELLS : EXPERIMENTAL PROTOCOL DEVELOPMENT
R ≈ 2-3 nm
70 um
2R ≈
10 um
VS
WHICH IS THE BEST PROBE?

## Slide 10
AFM & CELLS : EXPERIMENTAL PROTOCOL DEVELOPMENT
3d topo images
L. Puricelli et al.
“Nanomechanical and topographical imaging of living cells by Atomic Force Microscopy with colloidal probes"
Review of Scientific Instruments
Submitted on 16/09/14
Under revision

## Slide 11
AFM & CELLS : PROTOCOL TEST
EFFECT OF CYTOCHALASIN-D ON CELLULAR ELASTICITY
Cytochalasin -D : micotoxin which disrupts actin filaments network
cytoskeleton weakening, Young modulus decreases
after
before
Height
Young Modulus
nm

## Slide 12
AFM & CELLS : PROTOCOL TEST
EFFECT OF CYTOCHALASIN-D ON CELLULAR ELASTICITY
L. Puricelli et al.
“Nanomechanical and topographical imaging of living cells by Atomic Force Microscopy with colloidal probes"
Review of Scientific Instruments
Submitted on 16/09/14
Under revision
before
<E> = 235 ± 93 Pa
after
<E> = 142 ± 42 Pa

## Slide 13: AFM & CELLS : PROTOCOL APPLICATION
500 nm
X 104
CELLULAR DIFFERENTIATION INDUCED BY NANOSTRUCTURED SURFACES
24hr
X 104
Young Modulus
X 104
Flat Zirconia
24 hr
24 hr
Nanostructured zirconia
(15nm RMS roughness)
Height
X 104
X 104

## Slide 14: AFM & CELLS : PROTOCOL APPLICATION
nanostructured
zirconia (15nm rms)
Flat Zirconia +NGF
500 nm
CELLULAR DIFFERENTIATION INDUCED BY NANOSTRUCTURED SURFACES
C. Schulte, L. Puricelli et al.
“Nanoscale information of nanorough zirconia surface
favours neuronal differentiation by orchestrating
complex mechanotransductive events “
Under submission on “Journal of Cell Biology “
Nerve Growth Factor (NGF) VS Nanostructured Zirconia
Young modulus – cell body
The Young modulus of PC12 cells body is reduced on the nanostructured zirconia
nanostructured
zirconia (15nm rms)
Flat Zirconia +NGF
Young modulus – neurites

## Slide 15: CONCLUSIONS AND FUTURE PERSPECTIVES
Development and optimization of a common and robust methodology (covering all the steps of the experimental activity) for the AFM-based combined topographic/mechanical imaging of cells and tissues
Effective exploitation of AFM potentials in the biomedical field
Engineered nanostructured surfaces as cell culture plates for the study of the differentiation process
Applications of AFM in the fields of pre-diagnosis of cancer diseases, drugs testing, or regenerative medicine.

## Slide 16
THANK YOU FOR YOUR ATTENTION!

## Slide 17: AFM & CELLS : EXPERIMENTAL PROTOCOL DEVELOPMENT
FINITE THICKNESS EFFECT CORRECTION
Cell from HEK-293 line (human embryonic kidney)
 | Not-corrected | Corrected
Cell-body | 2.85 | 2.58
Lamellipodia | 3.56 | 2.82

## Slide 18: AFM & CELLS
Measuring cells’ nanomechanics - Why Atomic Force Microscopy ?
Standard tools in biology :
Compression between glass plates *
Micropipettes aspiration *
Tethers pulling with functionalized
microspheres or optical tweezers **
* A. Diz-Munoz et al. Trends in Cell Biology 23 (2013)
** A. D. Lieber et al. Current Biology 23 (2013)
Need of direct cytoskeleton elasticity measurements, provided with high spatial resolution and in one-to-one correspondence with topographic map
Low spatial resolution
Membrane surface tension: which linkage to membrane-cytoskeleton mechanical properties ?

## Slide 19
AFM & CELLS
Force spectroscopy
Force [nN]
Tip-sample distance [nm]
Adhesion
Approaching
Retracting

## Slide 20: OPEN PROBLEMS: 1) CONTACT MECHANICS MODEL (HERTZ)
MAIN LIMITS:
E ≈ constant (and scalar)
FA(δ) ≈ FR(δ)
δ , a << R
δ , a << h
Homogeneous and isotropic sample
Semi-infinite sample (negligible substrate
effect)
Purely elastic response
δ = sample indentation
δ0 = contact point
Fl = applied force
R = microsphere radius
σ = F/A (stress)
ε = strain (relative deformation)
Young modulus: intrinsic parameter! (not dependent on sample dimensions or shape)
Poisson coefficient = 0.5

## Slide 21
Dimitriadis correction (spherical probes)
Hertz
*[Dimitriadis et al. Biophys. J. 82:2798-2810 2002]
Opportunity to obtain mechanical properties from the whole cell surface :
Cytoplasmic protrusions (filopodia, lamellipodia), potentially rich in informations
On literature, data limited to the higher regions (nucleus) ≈ 10 % total surface area
Linearizable :
Opportunity to work in parallel on the whole force curves set (matrix linear regression)
Direct inspection of eventually different elastic regions (different slopes)
h
δ
δ << h
OPEN PROBLEMS: 3) FINITE THICKNESS EFFECT CORRECTION

## Slide 22
OPEN PROBLEMS: 4) MULTIPLE ELASTIC RANGES
INDENTATION RANGE SELECTION FOR YOUNG MODULUS FITTING
Complex problem:
Semi-automatic method: indentation percentages research
Hypothesis : local height is proportional to cytoskeletal components amount
thickness of cytoskeletal components
absolute indentation width of the different ranges
Strong hypothesis, need of manual check on a statistically significant force curves sample (≈ 50 -100)

## Slide 23
Strong adhesion
Weak adhesion
M. Indrieri et al., Rev. Sci. Instrum. 82 (2011)
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL

## Slide 24
COLLOIDAL SPHERICAL PROBES CHARACTERIZATION *
* M. Indrieri et al., Rev. Sci. Instrum. 82 (2011)
Reverse imaging
Radius fitting by means of spherical cap equations
Each spherical cap is independent: robust statistic
characterization
Appropriate filters to discarde images given by
damaged spikes
error ≤ 1%
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL

## Slide 25
FEATURES
Temperature control (36 ± 1 °C)
Transparent heater (good optical visibility)
Calibration curve : T = f (ΔV)
Plastic cap with an hole for AFM-head
(limiting culture medium vaporization)
tmax ≈ 5 h
3) TRANSFERRING IN A SUITABLE AFM THERMALIZED CELL (37°C)
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL

## Slide 26
5a) Contact point determination
Algorithm for:
Estimated error: dδ0 = ± 10 nm
Fast algorithm : about 1-2 mins for the whole force curves set
Fit on a suitable percentage of the cut-free indentation
region
Force curve cut (noisy non-contact region plus a small region
near the contact point) and linearization
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL

## Slide 27
5b) Real topography map build-up
Cell from MDA-MB-231 line (human breast cancer)
+
def.
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL

## Slide 28
5d) Young modulus total error estimate
Two main contributions:
Intrinsic variability of the bio-system (cell-by-cell differences)
Errors due to the measurement process on the single cell (experimental parameters uncertainties propagation and intrinsic variability of the single cell)
E1
E3
E2
EN
COMBINED TOPOGRAPHIC/MECHANICAL IMAGING PROTOCOL