## Slide 1: Time Resolved dynamics of La0.65Sr0.35MnO3 thin films

## Slide 2: Outline
My project
Experiments on La0.65Sr0.35MnO3
  What is La0.65Sr0.35MnO3?
Time resolved optical measurements
  Reflectivity
  Kerr effect

## Slide 3: Ultraspin endstation
A new laser beamline for time resolved photoelectron spectroscopy

## Slide 4: ULTRASPIN ENDSTATION
Vectorial
Spin-polarimeter
Sample Preparation chamber
Analysis
chamber
High spin polarization of the emitted electrons
Kinetic energy
EF
Number of electrons

## Slide 5: Experiments on La0.65Sr0.35MnO3

## Slide 6: What is La0.65Sr0.35MnO3?
Perovskite structure.
Itinerant ferromagnetism (double exchange).
J. Phys.: Condens. Matter. 25 136005 (2013)
J. Phys. D: Appl. Phys. 47 (2014) 034010.
Half metallic bandstructure, very high spin-polarization at the Fermi energy
Strong correlation between lattice structure, electronic structure and magnetic behaviour.

## Slide 7
Nat. Mat. 8, 56 (2008)
Number of electrons
Absence of final states for spin-flip scattering
Magnetic quenching is very slow with respect to metals
Ef
Ferromagnetic Metal
Half-metal

## Slide 8: Time resolved optical measurements
Reflectivity and magneto-optical Kerr effect measurements in pump-probe mode

## Slide 9: Optical measurements
Laser characteristics:
  High repetition rate (80 kHZ).
  Two colour (pump 1.55 eV, probe 3.1 eV).
  Pulse duration 70 fs FWHM.
Sample characteristics:
  LSMO (001) on SrTiO3 substrate, (1%) tensile strain.
  MBE grown (high purity, high crystalline quality).
  Transition from ferromagnetic metal to paramagnetic (higher-resistivity) metal at Tc=330 K.

## Slide 10: Reflectivity
Shock Wave (coherent optical phonon) interfering with probe.
Ultrafast conductivity change due to large excitation density (10-1 ph/Mn site)
Electrons equilibrate with lattice within 1ps

## Slide 11: MOKE measurements
Same timescales
Different amplitude
Coupling with phonon
Different timescales and amplitudes

## Slide 12: MOKE - Temperature
Critical slow-down occurs close to Tc as observed in T. Ogasawara et al. PRB 68, 180407 (R) (2003). Magnetization decay time increases.
Lattice heating
Of magnetic system
Electronic excitation
of magnetic system

## Slide 13: Results
0-5 ps timescale: We identified an ultrafast quenching in an half-metal, that must have purely electronic origin.
5-100 ps timescale: We identified a coupling between the coherent optical phonon and the magnetic response.
100-700 ps timescale: The behaviour agrees well with considerations based on the bandstructure.

## Slide 14: Open questions
0-5 ps timescale: How can we explain the ultrafast quenching? We need measurements that directly probe the electronic structure: Time-Resolved Photoelectron Spectroscopy.
5-100 ps timescale: What generates the coupling between the phonon and the magnetization? Is it possible to control it, p.e. with strain?

## Slide 15: Thank you for your attention!

## Slide 16: Acknowledgements
S. Günther, M. Kronseder, M. Büchner, H. Körner, Prof. C.H. Back
– My kind hosts in Regensburg Universität
A. Y. Petrov, B. Davidson
- Sample growth and characterization (transport, XRD)
G. Panaccione, G. Rossi

## Slide 17: Appendix
Useful tools

## Slide 18
Elettra Storage Ring
L. Pastrovicchio et al. Topolino 3070, 2
Linac Building Extension
Undulator Hall
Experimental Hall
New world of non-equilibrium phenomena
Extremely strong user selection

## Slide 19: High Harmonics Generation
Harmonics generation from a gas (Ar, Ne)
Gives ultra-short, coherent, soft-X ray photon pulses from a solid state laser
Low intensity
Can provide an intermediate step between the laboratory and the Free Electron Laser

## Slide 20
Pump Laser
Pharos 20W 400 µJ
Interaction Chamber
Monochromator and switch
Slits and Refocussing
ULTRASPIN
T-REX

## Slide 21: ULTRASPIN ENDSTATION
Vectorial
Spin-polarimeter
Sample Preparation chamber
Analysis
chamber

## Slide 22: Mott scattering
Spin dependence in scattering processes
Scattering Mott (1932):
Elastic electrons (40-200 keV)
Spin-orbit effect

## Slide 23: Mott Polarimeter
Sherman function
Stable
Two components of at a time

## Slide 24: TR-MOKE measurement set-up
BBO crystal generates the second harmonic (3eV) of the pump laser (1.5eV)
A delay line allows to remotely control the pump-probe delay
A chopper, connected to a lock-in allows to MODULATE the PUMP BEAM
Sample is magnetized and measured with applied field (saturation) in opposite directions
When dynamical hysteresis are measured, the blue beam is chopped.
When normalizationhysteresis are measured, the blue is chopped AND red is blocked.

## Slide 25: Magnetism characteristic lengths