## Slide 1: Electronic Properties of Low Dimensional Quantum Materials
C. Bigi

## Slide 2: OUTLINE
Motivations
Experimental techniques
Case study: Bi2Se3 thin films
Perspectives
APE BEAMLINE

## Slide 3: WHAT ARE WE LOOKING AT?
Many properties of solids are determined by electrons within a narrow energy slice around EF
E
EF
Metal
Semimetal
Semiconductor
Insulator

## Slide 4: NEW PHASES OF MATTER
2016

## Slide 5: WHY TOPOLOGICAL INSULATORS?
EF
SOC
Trivial insulator
Topological insulators possess robust metallic surface states with characteristic spin texture
NPG Asia Materials research highlight, 29 November 2010
Phys. Rev. B 84, 165113
(2011)
TRS
BZ
BZ
Topological insulator

## Slide 6: WHY TOPOLOGICAL INSULATORS?
SCIENTIFIC REPORTS | 2 : 726 | 2012

## Slide 7: PHOTOEMISSION SPECTROSCOPY
Conventional ARPES very few layers
Soft X-Ray ARPES “bulk” contribution
SARPES

## Slide 8: SPIN-RESOLVED ARPES: EXCHANGE SCATTERING
Exchange scattering
Very Low Energy Electrons Diffraction (VLEED)
ferromagnetic O2 passivated Fe(001) target grown on MgO substrate
6

## Slide 9: SPIN-RESOLVED ARPES: VESPA DETECTOR
Bigi C. et al, JSR, 24,4 (2017)
hv= 30 eV
Au(111)
S = 0.3 – 0.5
FOM = 3.3 · 10-2
VESPA: Very Efficient Spin
Polarization Analysis
hv= 50 eV
ΔE~ 70 meV
ΔE~ 100 meV

## Slide 10: PULSED LASER DEPOSITION TECHNIQUE
Manganites | Cuprates
La-Ba-Mn-O | Y-Ba-Cu-O
La-Ca-Mn-O | Other materials
La-Sr-Mn-O | La-Al-O
La-Ce-Mn-O | Sr-Ti-O
Sr-Mn-O | TiO2
Bi-Mn-O | Bi2Se3

## Slide 11: WHY THIN FILMS?
Zahid and Lake, APL 2010
D.G.Schlom’s group
ULTRA-thin layers
(e.g. single-unit or
sub-unit cell)
Substrate induced strain
(e.g. deformation and/or forbidden phases)
Orientation control
Tailored hetero-structures
(courtesy of Sara Orgiani)
D.G.Schlom’s group

## Slide 12: ARPES ON PLD Bi2Se3 THIN FILMS
hv = 55 eV

## Slide 13: SPIN-RESOLVED ARPES ON PLD Bi2Se3 THIN FILMS
Phys. Rev. B 84,
165113 (2011)
TRS
Orgiani P., Bigi C. et al, APL, 110, 171601 (2017)
hv = 55 eV

## Slide 14: SPIN-RESOLVED ARPES ON PLD Bi2Se3 THIN FILMS
EF
EF
Even in presence of slight Se off-stoichiometry, SARPES investigation shows the TSS are protected and not destroyed by any small source of chemical or structural disorder
Phys. Rev. B 84,
165113 (2011)
TRS
hv = 55 eV
-40 0 40

## Slide 15: PERSPECTIVES
Low deposition rate will allow the doping (e.g. Mn, Fe, Co) of the films in a large range of values
Heterostructures with HTC superconductors may pave the way to experimentally detect new physics
Nature 511, 449 (2014)
NanoLett 17, 3493 (2017)
High-pressure RHEED is currently under commissioning better control of film thickness and surface properties

## Slide 16: THANKS FOR YOUR ATTENTION
Acknowledgments
Growth + XRD + LEED
P.Orgiani, C.Bigi
ARPES + SpinARPES
C.Bigi, P.Kumar Das,
J.Fujii, I.Vobornik
XPS
P.Orgiani, C.Bigi,
B.Gobaut, P.Torelli G.Panaccione
PhD Supervisor
G.Rossi
Financial support
NOXSS-PRIN MIUR NFFA-MIUR

## Slide 18: GROWTH OPTIMIZATION: TEMPERATURE
STO substrate
T~290°C Bi2Se3
T~340°C Bi3Se4
T~400°C amorphous
v
QL
VdW
gap
SL
VdW
gap

## Slide 19: GROWTH OPTIMIZATION: PRESSURE
P = 10^-3 mbar
P = 10^-1 mbar
hv =500 eV
Ts = 290°C
Bi5d
Bi5d
Se3d
Se3d
Bi0
Bi0

## Slide 20: GROWTH – SrTiO3 (111) vs Al2O3 SUBSTRATES
The out-of-plane c-axis and the in-plane a-axis were found to be 2.858 nm and 0.422 nm, which indicates a slight tensile in-plane strain which elastically induce a reduction of the
out-of-plane cell elongation. (c=2.864 nm a=0.414 nm)

## Slide 21: GROWTH ON Al2O3 (0001) SUBSTRATE
laser fluence | 5 J/cm2
laser frequency | 1 Hz
substrate temperature | 290 ° C
Ar pressure | 10-1 mbar
growth rate | 0.07 nm/shot
Orgiani P., Bigi C. et al, APL, 110, 171601 (2017)

## Slide 22: PLD-GROWN BI2Se3 (001) THIN FILMS
Good surface quality on Al2O3(001) substrates
Absence of C and O contaminants
Absence of Bi or Se cluster aggregation
Orgiani P., Bigi C. et al, APL, 110, 171601 (2017)
XPS @ 920 eV
laser fluence | 5 J/cm2
laser frequency | 1 Hz
substrate temperature | 290 ° C
Ar pressure | 10-1 mbar
growth rate | 0.07 nm/shot

## Slide 23: SPIN-RESOLVED ARPES: VESPA DETECTOR
Bigi C. et al, JSR, 24,4 (2017)
Very Low Energy Electrons Diffraction (VLEED)
ferromagnetic O2 passivated Fe(001) target grown on MgO substrate
Ek = 90 eV
Operates @ Ek = 6 eV
Okuda et al. Rev. Sci. Instrum. 79, 123117 (2008); Bertacco et al. APL (1998)

## Slide 24: EXCHANGE SCATTERING: Fe(001)-p(1x1)-O TARGET
Okuda et al. Rev. Sci. Instrum. 79, 123117 (2008); Bertacco et al. APL (1998); Rev.Sci.Instrum.(1999); Pincelli Master thesis

## Slide 26: TOPOLOGY IN BAND THEORY

## Slide 27: TOPOLOGY IN BAND THEORY

## Slide 28: TIME REVERSAL SYMMETRY