## Slide 1: Delayed creep of weak gels. A microrheological investigation.
Paolo Edera
Complex Fluids and Molecular Biophysics Lab
UNIMI PhD School

## Slide 2: Delayed creep of weak gels. A microrheological investigation.
creep compliance
WHAT IS GOING ON DURING DELAY TIME?
WHAT HAPPENS TO THE MATERIAL JUST BEFORE IT BREAKS?
HOW DOES THE MATERIAL KNOWS IT HAS TO BREAK?
ARE THERE ANY PRECURSORS TO THE MATERIAL FAILURE?
Notes: Material’s mechanical characteristics are encoded in this function called creep compliance.
Several question arise concernig this phenomenon:
Is J caracteristic of the unperturbed system?
Or J depends on the stress \sigma?
changes because of the application of a stress
In other words, can the creep time be predected by some unperturbed state characteristic?
Material’s mechanical characteristics are encoded in this function 𝐽 called creep compilance.
Several question arise concernig this phenomenon:
Is J caracteristic of the unperturbed system?
Or J depends on the stress \sigma?
changes because of the application of a stress
In other words, can the creep time be predected by some unperturbed state characteristic?

## Slide 3: Delayed creep of weak gels. A microrheological investigation.
This phenomenon is common to a wide class of materials
metals
Earth’s crust
paintings

## Slide 4: Delayed creep of weak gels. A microrheological investigation.
Liquid phase
Solid phase
Liquid phase
Solid space-spanning network
Gels can be divided in
STRONG if network energy per bond
and
WEAK if network energy per bond
What’s a Gel?
Gel is a two phases material

## Slide 5: Delayed creep of weak gels. A microrheological investigation.
Notes: Gels often combines advantageous features of liquids, in applicability, and solids in ‘stability’

## Slide 6: Delayed creep of weak gels. A microrheological investigation.
Notes: Si forma un sistema eterogeneo con una fase solida (vetrosa) e una fase liquida

## Slide 7: Delayed creep of weak gels. A microrheological investigation.
We are dealing with very fragile materials
Weak gels
Traditional mechanical methods are not sensitive enough
estensometer
rheometer

## Slide 8: Delayed creep of weak gels. A microrheological investigation.
Brownian motion can help us!
Relation between position-fluctuation and creep compliance
In the simple case of newtonian fluids it reduces to
number of dimensions
fluid viscosity
particle’s radius

## Slide 9: Delayed creep of weak gels. A microrheological investigation.
sample
tracers
capillary
microscope
videocamera
Frame rate
Notes: Please note that tracers can be smaller than optical resolution limit, and there is no need to resolve them individually

## Slide 10: Delayed creep of weak gels. A microrheological investigation.
Time evolution of correlation is conveniently studied in the Fourier domain
The correlation between images at a given temporal delay contains the information about tracers’ mean square displacement.
Gaussian displacement distribution
Notes: Since the particle concentration corralation in the fourier domain is by definition the fourier transorm of the displacement probability distribution

## Slide 11: Delayed creep of weak gels. A microrheological investigation.
From a single experiment (a single stack of images) are obtained several independent correlation functions
Differential Dynamic Microscopy

## Slide 12: Delayed creep of weak gels. A microrheological investigation.
This self consistent procedure aloud to measure msd
with no a priori assumption on it’s functional form
Inversion problem:

## Slide 13: Delayed creep of weak gels. A microrheological investigation.
Water and glycerol mixtures
Polymeric Solution in semi-diluted regime (PEO 2MDa 2% wt)

## Slide 14: Delayed creep of weak gels. A microrheological investigation.
Completed tasks:
  Extended DDM to micro rheology
  Not Discussed
  Identified and removed artefacts due to:
    Finite exposure time
    Finite size images
Next steps:
  Apply DDM microrheology to gels with and without external load
  Possible heterogeneity
  Possible violation of gaussian displacement distribution hypothesis

## Slide 15: Delayed creep of weak gels. A microrheological investigation.
Grazie per l’attenzione

## Slide 16: Delayed creep of weak gels. A microrheological investigation.

## Slide 17: Delayed creep of weak gels. A microrheological investigation.
Microrheology
J(t) is the creep compilance: the time dependent strain following a suddenly applied weak shear stress.

## Slide 19: Delayed creep of weak gels. A microrheological investigation.
}
=